# Lecture 28 Rigid Pavements

General discussion related to design method and cracking control and stress in concrete pavements.

# Types of concrete pavement

Unreinforced jointed concrete pavement - PJCP

# Reinforced jointed concrete pavement - RJCP

Continuos concrete pavement - CRCP

Slab design - Stress due to loads determined by beam on elastic foundation techniques

Cracks are going to occur and are controlled by joints, temperature steel and load transfer devices

# Stresses

Load - basically from bending conditions and take the form

In general as

# P is the applied load and h is the pavement thickness

Or for specific applications something like

l is the radius of relative stiffness and b is the relative radius of the load

Temperature stress - related to differential in temperature between top and bottom of the slab from plate theory

when substitute into the bending stress equation

produce

e is the coefficient of thermal expansion, t is the temperature differential and E is the modulus of elasticity of concrete.  This equation is from plate theory

Crack control is related to the type and spacing of the joints.  Typically is short spacing for PJCP and longer spacing for RJCP.  Both types have load transfer devices along the joint to prevent joint destruction and eliminate pumping of the sub grade materials.  Typical joints and spacing patterns are available from MDOT Standard Plans.

Pavement Design