# Lecture 31 AASHTO Design Method

# This method developed out of the AASHTO road test in the 1960s and has been refined several times. AASHTO Design Guide .  The equation from the 1986 Guide is

# where

# ZR = Standard normal variant

# So = overall standard deviation

# W18 = 18 kip ESAL

# D= thickness in inches

# DPSI = serviceability loss

# Pi = initial serviceability

# Pt = final serviceability

# Ec = elastic modulus of concrete

# Sc = modulus of rupture of concrete

# J = load transfer coefficient = 3.2 (assumed)

# Cd = drainage coefficient

# K = modulus of sub grade reaction

Data needed to solve the equation for pavement thickness.

# Change in performance, (PSI usually 2 to 2.5

Modulus of sub reaction Modulus of Sub Grade Reaction Test

# Requires corrections for

Seasonal effects

# Thickness of sub base

Loss of support

# Location of bedrock

Traffic – by ESAL

Concrete properties

# MOR-varies with concrete mix in the range from 500-800 psi

# Modulus of elasticity- typical value 4000000 psi

Drainage coefficient as in the flexible pavement design

Reliability- depends on the functional classification 50%-99.9%

Standard deviation-0.4 to 0.5

Load transfer – RJCP = 3.2, PJCP = 3.8

# Loss of sub grade support

CTB = 0 to 1

Granular = 1 to 3

Fine granular = 2 to 3

Solution to equation shown in AASHTO Design Guide for Pavement Structures or Fig 21.13

A Calculator for determining concrete pavement thickness is available at Calculator for Concrete Surfaced Road