# Lecture 25 Thickness of Flexible Pavement Components

The AASHTO flexible pavement design procedure results in the equation

the a's are material coefficients, D's are depth of the layers (inches) and m's are the drainage coefficients

The solution to this equation requires some assumptions and is done in a successive manner from the top layer (Asphalt) to the bottom layer (Subbase).

# Example follows

Given:

# ESAL = 5x106

Mr. Asphalt = 450000 psi

# Mr. Base  = 20000 psi

Mr. Subbase = 10000 psi

# Mr.  Subgrade = 5000 psi

Reliability = 95%

m2=1.0

m3=0.8

# Standard deviation = 0.35

(PSI = 4.2-2.5=1.7

Calculation of layer thickness can be determined from the structural number, SN.

# Asphalt Layer Use Mr. = 20000

# Base Layer Use Mr. = 10000

# Sub base layer Use Mr.  = 5000

Therefore the SN = .44x7+.14x4x1.0+.11x15.5x.8=5.0=>5.0 required.

For a single layer system the SN is determined using the Mr of the sub grade Mr = 5000

This assumes that no base is used for drainage purposes.  Usually at least 4 in of aggregate is required for this purpose.

For a two layer system start wit Mr = 20000 psi for the base

Base layer calculated using Mr = 5000

Assuming the relative cost of the materials are

Asphalt = $2.00/in

Base Agg = $1.50/in

Sub base = $0.50/in.

The costs of the various alternatives are

Asphalt = 11.5x$2.00=$23

Asp + Base = 7x$2.00+14x$1.50 = $35

Asp + base +sub base=7x$2.00+4x$1.50+15.5x$0.50=$27.75

The least expensive alternative is the single layer assuming there is no requirement for drainage material under the asphalt.

A Calculator for determining asphalt road thickness is available at

Calculator for Asphalt Surfaced Road